| VIKTOR HLAVICKA Civil Engineering training BSc, 9. semester Budapest University of Technology and Economics Faculty of Civil Engineering | MÁTÉ TÓTH Structural Engineering BSc, 9. semester Budapest University of Technology and Economics Faculty of Civil Engineering |
| --- | --- |

Supervisors:

Éva Lublóy Assistant Professor, BME ÉŐK

Ákos Török Associate Professor, BME ÉŐK

Szabolcs Kovács-Sebestény Sales manager, Fischer Hungary LPs.

Experimental investigation of post-installed anchors, pull-out tests from concrete and natural rock specimens

The design method and basic design parameters of applying expansion and bonded anchors for concrete is
thoroughly studied. To the contrary, there are still uncertainties related to the usage and application of
anchors for rock that has an inhomogeneous nature.

Mostly, a local „in-situ” pull-out test is required before fixing into rocks or fix rocks, therefore the
appropriate anchorage could be determined –including the embedment depth and load transfer type - in
accordance to the current conditions. This fact indicates the importance of giving valuable results for
rocks and predicting the behavior of these steel-rock connections.

In this experimental study, a torque controlled expansion anchor (fischer FBN II 8/50) as well as bonded
anchors (fischer FIS V – vinyleaster, fischer FIS EM-epoxy) with Ø8 threaded rod were tested. The
embedment depth was 50mm. Two types of freshwater limestone (Süttő/Hungary), granite
(RosaBeta/Hungary) and even five different strength classes of concrete (C20/25, C25/30, C40/50,
C45/55, C55/67) were investigated. 93 pull-out tests were carried out focusing on the application of
tension stress, the displacement related to the punching force, and even the deformation of surface was
measured near to the fixing point. The tests were implemented in two series on rocks – normal conditions
and after a 50 cycle freeze-thaw test.

The relationship between the compressive-, flexural-tension strength values and the critical punching
force for concrete do not show the same trend as the ones of rocks. This study calls the attention to the
importance of porosity on the performance of the anchorages.