| ESZTER BOKÁNYI Physics BSc BSc, 5. semester Eötvös Loránd University Faculty of Science |  |
| --- | --- |

Supervisor:

Fanni Misják research fellow, Hungarian Academy of Sciences Research Centre for Natural Sciences Institute for Technical Physics and Materials Science

Phase separation in alloy nanoparticles

In technological application of nanostructures it is generally required that multiple, self-organising processes take place at only one technological step, establishing multifunctional structures. To understand these multicomponent, self-organising structures, phase separation processes must be carefully examined. Processes occuring at the first stages of vapor or solution deposition of nanoparticles are hardly or not at all observable; however, after examination at an atomic level one can draw conclusions on the entire process.

In order to be able to examine phase separation, we were aiming for a model system where simultaneous deposition causes metastable structures. This is the reason for choosing the Cu-Ag system, which has a wide miscibility gap.

Cu-Ag nanoparticles were created in several compositions (30-80 at.% Ag) by magnetron sputtering on a thin carbon substrate, with 8e-8 mbar background vacuum. The effective thickness of the films were 1-2 nm, the diameter of the particles was in the range of 2-20 nm.

With the help of high resolution electron microscopy, I examined the morphology, surface and internal structure of the generated particles. One-phase particles (possibly single crystals or multiply-twinned crystals) could be indentified; moreover, at some special compositions I found evindence of double-phase nanoparticles, and that of spinodal decomposition.

My results therefore showed that phase separation processes can begin even at the 2-3 nm size range.