| AGOST GYULA TASI Chemist MSc, 7. semester University of Szeged Faculty of Science and Informatics |  |
| --- | --- |

Supervisors:

Dr. Pál Sipos Associate professor, SZTE TTIK

Dr. Attila Pallagi Research fellow, SZTE TTIK

Condensation-type complex formation reaction of Al(III) with gluconate in solutions related to the Bayer-process

D-gluconate (Gluc−) is a known poison in the crystallization of gibbsite in Bayer-type, strongly alkaline solutions (Chem. Eng. Res. Des, 74, 1996 828.). Another paper (Polyhedron, 27, 2008 118–124.) claims that in these caustic systems there is no interaction between the Gluc– and the Al(III) complexes being present in the solution.
Interaction between Al(OH)4− and Gluc− in strongly alkaline solutions was confirmed unambigously via multinuclear NMR measurements, since the 27Al NMR peak referring to Al(OH)4− merges to the baseline with the systematic raise of Gluc− concentration. Determining the freezing-point depression confirmed the complexation between these two particles as well. In contrast to those described before, the pH potentiometric titrations (together with the published data; Polyhedron, 27, 2008 118–124.) do not refer to the complexation of the compounds in pH ≥ 12 solutions. Further 1H NMR measurements were performed at three different total NaOH concentrations ([OH–]tot = 0.500; 1.000; 1.667 M) to reveal the stability constant of the complex. Fitting of the integrated peaks associated with the complexed ligands resulted in the formation of a 1:1 ratio complex, with (estimated) stability constant of log k1,1 = 2.5 ± 0.5. This value was also confirmed via polarimetric measurements ([OH–]tot = 0.250 and 0.650 M; I = 1.00 M, NaCl). These results show that in strongly alkaline solutions, complexation is a pH-independent process, in other words, condensation reaction takes place. This hypothesis also agrees with Raman spectrometric and conductometric measurements.
UV-Vis spectrophotometric measurements attest that the carboxylate group of the Gluc– was not involved in the Al(OH)4− binding. The temperature-dependent 1H NMR measurements showed that the alcoholate groups on the 2nd and 3rd C-atoms were likely to coordinate to the Al(OH)4−. Analogously, the assumed structure of the “AlGluc” complex, forming in strongly alkaline solutions, was given as of tetrahedral geometry.