| DANIEL PETER KOROM Mechatronics Engineering BSc, 4. semester Óbuda University Donát Bánki Faculty of Mechanical and Safety Engineering |  |
| --- | --- |

Supervisors:

dr. Pal RACZ Associate Professor, OE BGK

András Szalay researcher engineer, S-Metalltech 98 Kft.

Tube forming with explosion

There is a special option to form high strength material: the forming with explosion. This
technology is a part of high energy rate forming technologies: during the explosion materials
transform in a very short time, and that follows the increase of pressure. We can use this
increased pressure for material forming, especially for sheet metal forming.

But here is around a bit different thing. In the middle of our project stands the tube forming.
Theese tubes are special: there are trough the length at determined diameters special forms.
The application of theese tubes takes place in metallurgy factories’ cooling systems.
Thatswhy the forms play a main role in the optimalization of colling systems, because they
transform the laminar flow to turbulent, and increase the efficiency of the system.

First of all: it is a very important point of view we would like to make seamless tube. It is not
a big deal to make this product from two halfs, and then weld the parts. But we had to find a
new methods of forming: there is an option: forming with explosion. We need a special tool
of course, which constains the negative form of our wanted tube. We put the unformed tube
into that, than we pulled an explosive wire through the tube, and it was filled with water.
After isolation we were ready for explosion.

But there is a couple of question: what is the influence of explosion to the structure of the
material? Is there any possibility of damage? Is there any special mechanical transformation?
To answer theese questions we have made some material researchs: hardness measuring and
wall wide measuring.
From the result we can see: the deformation of the material was very huge: the hardness
increased 20%, and the wall wide decresed 17% but the material solved this technology
without any major damage.

Before the industrial application we must make more researches and we must answer some
economical questions also. But they could be a theme of another scientific work.