| ATTILA BALINT Mechanical engineering BSc, 5. semester Budapest University of Technology and Economics Faculty of Mechanical Engineering | ZSOLT FERENC KOVACS BSc in Mechanical Engineering BSc, 5. semester Budapest University of Technology and Economics Faculty of Mechanical Engineering |
| --- | --- |
| ATTILA SZLANCSIK Mechanical engineering BSc, 5. semester Budapest University of Technology and Economics Faculty of Mechanical Engineering |  |

Supervisors:

Kornél Májlinger, PhD Assistant Professor, BME GPK

Imre Norbert Orbulov, PhD Assistant Professor, BME GPK

Mechanical properties of metal hollow sphere reinforced metal matrix syntactic foams

Metal matrix syntactic foams were produced. Reinforcement was pure iron hollow

sphere, the matrix materials were Al99,5 AlSi12, AlMgSi1 and AlCu5 alloys. The

volume fraction of the reinforcing hollow spheres were maintained at ~65 vol%.

The composites with AlMgSi1 and AlCu5 matrix material were tested under two

heat treatment conditions, half of the specimens were: annealed and the other half

precipitation heat treated. Compression tests were made immediately after the heat

treatments according the DIN 50134 standard by three height/diameter ratios (H/D=1,

1.5, 2) 6-6 samples from every composite and ratios respectively.

The structural stiffness, plateau strength and the total absorbed energy values increased

with higher H/D ratios, the absorbed energy values till 1% plastic deformation decreased.

The yield strength values of the composites varied between ~ 30-80 (MPa), the smallest

strength values had the samples with the Al99,5 matrix the highest the samples with the

precipitation heat treated AlCu5 matrix material. The structural stiffness values of the

composites varied between ~1000-7000 (MPa). The bonding and interface layer between

the spheres and the matrix material was also investigated with energy dispersive x-ray

spectroscopy and was found to be between 6-12 μm thick for all the samples respectively.