| BALAZS BRODA Chemistry BSc, 3. semester Eötvös Loránd University Faculty of Science |  |
| --- | --- |

Supervisor:

George Inzelt professor, ELTE TTK

Preparation and Characterization of Poly(5-aminoindole) by using Electrochemical Quartz Crystal Nanobalance Technique

Keywords: 5-aminoindole; electropolymerization; electrochemical quartz crystal nanobalance; overoxidation

The electrochemical quartz crystal nanobalance (EQCN) was employed to study the electropolymerization of 5-aminoindole on platinum electrodes in acidic media.

Potentiostatic or potential cycling electrooxidation of 5-aminoindole below 0.62 V vs. SCE leads to the formation of uniform, yellow, electrochemically active polymeric films. A scheme of the redox transformations of poly(5-aminoindole) which involves protonation-deprotonation steps accompanying the electron transfer is suggested.

At higher positive potentials, further oxidation takes place resulting in different blue-purple, indigo-type materials which remain attached to the metal surface but show decreased or no redox activity.